## Slide 1: Basic electron scattering theory and introduction to MULTEM
Zezhong Zhang
EMAT, University of Antwerp
STEM group, University of Oxford
27. 07.2020

## Slide 2
Outline
Electron wave function
Solving the scattering : Schrodinger equation
Multislice representation
  Weak-phase object
  Fresnel propagation
Sampling
  Potential sampling
  Probe sampling
Hand-on to MULTEM
  Probe
  Sample
  STEM simulation
  4D-STEM simulation
  Many more (depending on time)

## Slide 3
wave
Sampling
MULTEM
Multislice
Schrodinger

## Slide 4: Electron as wave
Wave from stationary observer
Wave equation
General solution

## Slide 5: Quantum mechanical wave
Intensity
Normalisation
Expectation of operator
Superposition

## Slide 6: Apply to electron microscopy
Schrodinger equation
Relativistic mass and wavelength correction
In vacuum
In specimen
Time-dependent
Time-independent

## Slide 7: Multislice solution
Schrodinger equation
Wave function vary slow in z
Incident kinetic energy

## Slide 8: Multislice solution
Solution
Transmission function
Fresnel propagator
weak phase object
propagate
detailed derivation in supplementary

## Slide 9: Potential sampling
Pixel size = real space length / # pixels
Max scattering vector
To avoid aliasing, take bandwith limit to the 2/3 of the max scattering vector.
Allowed angle
Thus, Pixel size = wavelength/ 3 / max scattering angle

## Slide 10: Probe sampling
Diffraction-limited resolution
The Nyquist-Shannon sampling theorem
probe step size =

## Slide 11: Frozen phonon
Einstein model
Each atom oscillate independently
Why frozen? Atoms are slow!
The electron pass your sample in 10^-15~10^-16 s while atom vibrate 10^-12~10^-13 s
Mean displacement and rms3d
rms3d = sqrt(<u^2>)
Check for Debye-Waller factor: Peng, L. M., Ren, G., Dudarev, S. L., & Whelan, M. J. (1996).. Acta Cryst. A 52(3), 456–470.

## Slide 12: Supplementary: Derivation of multislice
Reference:
Kirkland, Earl J. Advanced computing in electron microscopy. 2nd ed.
New York: Plenum Press, 2010.

## Slide 13: Multislice solution
Schrodinger equation
Wave function vary slow in z
Incident kinetic energy

## Slide 14: Multislice solution

## Slide 15: Multislice solution

## Slide 16: Multislice solution

## Slide 17: Multislice solution

## Slide 18: Multislice solution

## Slide 19: Multislice solution

## Slide 20: Multislice solution

## Slide 21: Multislice solution

## Slide 22: Practical on MULTEM image simulations software EMAT workshop 2019
Courtesy:
Dr. Ivan Lobato
Annelies De wael
Thomas Friedrich

## Slide 23
Why do we need simulations?
The quantum mechanical nature of the electron-specimen interaction requires that the experimental data must be compared and complemented by numerical simulations.
HRTEM SrTiO3[110]
Experimental
Simulation
STEM Au nanorod[110]
Experimental
Atom counting

## Slide 24: How to perform accurate and fast simulations?
High-energy Schrödinger equation
Multislice method
Bloch method
Linear superposition
DFT
Specimen potential

## Slide 25: How to perform accurate and fast simulations?
High order expansions of the multislice solution of the high-energy Schrödinger equation,
accurate electron scattering parameterization,
correct subslicing of the 3D atomic potential,
frozen phonon/atom calculations,
proper inclusion of the microscope aberrations,

## Slide 26: How to perform accurate and fast simulations?
  GPU technology,
  Multithreading,
  C++/Cuda C++,
  C++ Lib., Matlab and GUI.

## Slide 27: MULTEM graphical user interface
Header
  Reset parameters to default values
    At the start of each exercise in this tutorial
  Run simulation
  Stop simulation
4 input screens
  General settings
  Specimen
  Experiment
  Microscope settings
Simulated image opens in new window

## Slide 28
https://github.com/Ivanlh20/MULTEM
MATLAB
GUI

## Slide 29: General settings
MATLAB
GUI

## Slide 30: Simulate the electron beam
We start without a sample by choosing simulation type “IWRS”

## Slide 31: Exercise 1: Acceleration voltage
80 kV
300 kV

## Slide 32: Exercise 2a: Defocus
defocus = -100 Å
Defocus (Scherzer) = -14.03 Å
defocus = 100 Å

## Slide 33: Exercise 2b: Spherical aberration
Cs = 0.01 mm, Scherzer defocus -44.4 Å
Cs = 0.1 mm, defocus -44.4 Å
Cs = 0.1 mm, Scherzer defocus -140.4 Å

## Slide 34: Exercise 2c: Two-fold astigmatism
C12 = 20 Å: module
C12 = 20 Å: phase

## Slide 35: Exercise 2c: Two-fold astigmatism
C12 = 20 Å, φ12 = 45°: module
C12 = 20 Å, φ12 = 45°: phase

## Slide 36: Exercise 2d: Three-fold astigmatism
C23 = 25000 Å: module
C23 = 25000 Å: phase

## Slide 37: Exercise 2e: Coma
C21 = 25000 Å: module
C21 = 25000 Å: phase

## Slide 38: Apertures
(c)

## Slide 39: Exercise 3a: Aperture outer radius C30 = 0.001mm C10 = -14.03Å and C12 = 0.0Å
7 mrad
21 mrad
50 mrad

## Slide 40: Exercise 3b: Aperture outer radius C30 = 0.001mm C10 = -14.03Å and C12 = 20Å
7 mrad
21 mrad
50 mrad

## Slide 41: Aperture inner radius – Bessel beam

## Slide 42: Exercise 4: Aperture inner radius – Bessel beam
Module
Phase

## Slide 43: Exercise 5a: Vortex beam
m = 0: module
m = 0: phase

## Slide 44: Exercise 5b: Vortex beam
m = 1: module
m = 1: phase

## Slide 45: Exercise 5c: Vortex beam
m = 2: module
m = 2: phase

## Slide 46: Introducing a sample in our simulations
Simulating interactions with the specimen
For speed, we work with simulation type “EWRS”

## Slide 47: Electron specimen interaction
MATLAB
GUI

## Slide 48: Exercise 6: Electron specimen interaction
Multislice approximation
Weak phase object approximation

## Slide 49: Exercise 6: Electron specimen interaction
Phase object approximation
image intensity
Phase object approximation
phase
10-16

## Slide 50: Extra information: electron scattering parameterization
MATLAB
GUI

## Slide 51: Exercise 7: Electron phonon interaction
GUI
MATLAB
e-phonon interaction
Single image configuration
average image

## Slide 52: Specimen specific simulation settings
For speed, we still work with simulation type “EWRS”

## Slide 53: Exercise 8: Adding vacuum
Without recentering
With recentering

## Slide 54: Exercise 9: Rotation
Rotation of crystal does not change zone axis orientation
Rotation of nanocrystal

## Slide 55: Exercise 10: Crystal by thickness

## Slide 56: Exercise 11: Defocus
Zero defocus at last atom
Zero defocus at first atom
Zero defocus at middle of specimen

## Slide 57: Exercise 12: Potential slicing
MATLAB
GUI

## Slide 58: Exercise 12: Potential slicing
Slicing by dz slice thickness 2Å
Slicing by dz slice thickness 20Å
Slicing by planes

## Slide 59: Exercise 13: Sampling
Nx = Ny = 128
Nx = Ny = 1024

## Slide 60: Different imaging modes
Only a limited introduction, due to calculation time

## Slide 61: Exercise 14: High resolution transmission electron microscopy

## Slide 62: Exercise 15a: Diffraction spots

## Slide 63: Exercise 15b: Kikuchi lines

## Slide 64: Exercise 16: STEM
5 scan points
20 scan points

## Slide 65: Exercise 16: STEM
10 scan points, detector 1
40-100 mrad
10 scan points, detector 20-20 mrad

## Slide 66: Exercise 17: EFTEM
Sr, energy edge 1940
O, energy edge 532

## Slide 67: Questions?